## Slide 1: Superpave Study Group
Math

## Slide 2: Summary
Gmb – Bulk Specific Gravity of compacted asphalt sample. (T166)
Abs - Absorption
Gmm – Maximum Specific Gravity of Loose Mix Asphalt. (T209)
Va – Air Voids of a compacted asphalt sample. (T269)
Gse – Effective Specific Gravity of Aggregate.
VMA – Percent Voids in Mineral Aggregate.
Gsb – Bulk Specific Gravity of the combined Aggregate.
VFA – Percent Voids filled with Asphalt

## Slide 3
Gsb

## Slide 4: 1. Bulk Specific Gravity (Gmb)
Determine the Gmb of the compacted specimen:
  Dry Mass 4555.6 g = A
  SSD Mass _ 4562.4 g = B
  Submerged Mass 2620.0 g = C
Formula to use:
Round to nearest 0.001

## Slide 5
ANSWER #1
4555.6
(4562.4 – 2620.0)
4555.6
1942.4
2.3453
2.345

## Slide 6: 1b. Bulk Specific Gravity (Gmb)
Determine the Gmb of the compacted specimen:
  Dry Mass 4548.2 g = A
  SSD Mass 4551.9 g= B
  Submerged Mass 2615.8 g= C
Formula to use:
Round to nearest 0.001
Gmb = 2.355

## Slide 7
4548.2
(4551.9 - 2621.0)
4548.2
1930.9
2.35548
2.355
=
=
ANSWER #1b

## Slide 8: 2. % Absorption (Abs)
Determine the % absorption of a compacted specimen:
  Dry Mass 4573.6_ g = A
  SSD Mass _ 4585.1_ g = B
  Submerged Mass 3633.0 g = C
Formula to use:
Round to nearest 0.01%
% Abs =
X 100
Note: AASHTO T166 states if the % Absorption is greater than 2%,
Gmb for the specimen is not valid, an alternative Method can be use:
AASHTO T275 or AASHTO T331.

## Slide 9
ANSWER #3
Absorption =
ANSWER #2

## Slide 10: 2b. % Absorption (Abs)
Determine the % absorption of a compacted specimen:
  Dry Mass 4555.2_ g = A
  Submerged Mass _ 4567.6_ g = B
  SSD Mass 2615.3 g = C
Formula to use:
Round to nearest 0.01%
% Abs =
X 100
Absorption = 0.64%

## Slide 11: 3. Maximum Specific Gravity (Gmm)
Determine the Gmm of a loose mix (RICE)
  Dry Mass 1785.4_ g = A
  Submerged (Rice + Bowl) Mass _ 2358.6_ g = C
  Submerged Bowl Mass 1325.0 g = C
Formula to use:
Round to nearest 0.001
Gmm =
X 100
2358.6 – 1325.0 C = 1033.6
1033.6g

## Slide 12
ANSWER #3

## Slide 13: 3b. Maximum Specific Gravity (Gmm)
Determine the Gmm of a loose mix (RICE)
  Dry Mass 1806.2_ g = A
  Submerged (Rice + Bowl) Mass _ 2349.9_ g = C
  Submerged Bowl Mass 1315.0 g = C
Formula to use:
Round to nearest 0.001
Gmm =
X 100
2349.9 – 1315.0 C = 1034.9
1034.9g
Gmm = 2.342

## Slide 14
ANSWER #4
ANSWER #4b

## Slide 15: 4. Effective Specific Gravity of Aggregate (Gse)
The ratio of weight oven dry aggregate
To the volume of aggregate plus
Permeable pores that not absorbed
With asphalt, at a stated temperature.

## Slide 16: 4. Effective Specific Gravity of Aggregate (Gse)
Determine Gse of the mixture.
Pb = 4.8 %
Gmm = 2.358
Gmb = 1.038
Formula
Round to nearest 0.001

## Slide 17
ANSWER #5

## Slide 18: 5b. Effective Specific Gravity of Aggregate (Gse)
Determine Gse of the mixture.
Pb= 5.7 %
Gmm= 2.413
Gbulk= 1.032
Formula
Round to nearest 0.001
Gse = 2.625

## Slide 19: 6. Calculate Voids in Mineral Aggregate (VMA).
Determine % VMA of the mixture.
Ps= 94.0%
Average Gmb = 2.304
Gsb = 2.612
Formula
Round to nearest 0.1%

## Slide 20
ANSWER #6

## Slide 21: 6b. Calculate Voids in Mineral Aggregate (VMA).
Determine % VMA of the mixture.
Ps= 94.02%
Average Gmb = 2.411
Gsb = 2.708
Formula
Round to nearest 0.1%
Gse = 16.29% = 16.3%

## Slide 22: 7. Calculate the combined (weighted average)Gsb of the aggregate blend shown on the JMF on the next slide.
Determine Gsb of the mixture.
Formula =
Round to nearest 0.001
P = % of each aggregate
Gsb = Bulk specific gravity of each aggregate

## Slide 23
64.0 11.0 22.0 3.0
64.0 11.0 22.0 3.0
2.512
2.425
2.418
2.288

## Slide 24
ANSWER #7

## Slide 25: 7b. Determine the Gsb of this mixture…
Gsb = 2.560

## Slide 26: 7. Calculate the percent voids filled with asphalt, VFA.
Determine VFA of the mixture.
Formula = VFA, % = 100 X
Round to nearest 0.1
Va = % Voids in Total Mix = 3.8%
VMA = Percent voids in Mineral Aggregate = 14.8%
( VMA – Va )
VMA

## Slide 27
ANSWER #7
Round to nearest 0.1